Physical Properties of Burke Field Sheet (0.045” Nominal)

Membrane is 0.045 in. nominal thickness, scrim reinforced, uncured (thermoset) CSPE

| Property | Test Method | Minimum Spec.* | Typical Avg. Values |
| --- | --- | --- | --- |
| Thickness: - Total overall (mils) - Min over scrim (mils) Test Properties * (each direction) 1. Breaking Strength (pounds) Machine Direction Cross Direction 2. Elongation at Break Machine direction Cross direction Tear Propagation (pounds) Machine direction Cross Direction Hydrostatic Resistance Puncture Resistance Bonded Seam Strength Ply Adhesion (lbs./in. width) Ozone Resistance ** Low Temperature *** | ASTM D751 Optical Method ASTM D751 Grab Method ASTM D751 Tongue Tear (8 x 8 sample) ASTM D751 Method A Procedure 1 FTMS 101B Method 2031 ASTM D751 Modified (12 in./min) ASTM D413 Machine Method, Type A (12 in./min.) ASTM D1149, 1/8” Bent loop, 100 pphm 104 deg. F., 7 days ASTM D2136, 1/8” Mandrel 4hrs. @ -40 deg. F. | 41 mil 11 mil 250 lbs. 60 % 80 lbs. 350 psi 225 lbs. 225 lbs. 8 lbs. No affect Pass | 45 nom. Pass 320 lbs. 340 lbs. 105% 105% 115 lbs. 100 lbs. 425 psi 275 lbs. 90% of parent material 10 lbs. Pass Pass |

*Reference Burke Industries specification for interpretation of D751 test results.

** Low Temperature D2136 results were determined from base formula and is not repeated.

*** Ozone resistance D1149 results were determined from base formula and is not repeated.